# Sr3MO4F (M=Al, Ga)—A New Family of Ordered Oxyfluorides

Authors: Vogt T.1; Woodward P.M.2; Hunter B.A.3; Prodjosantoso A.K.4; Kennedy B.J.4

Physics Department, Brookhaven National Laboratory, Upton, 11973-5000, New York 2: Chemistry Department, Ohio State University, Columbus, Ohio, 43210-1185 3: ANSTO, Lucas Heights, NSW, 2234, Australia 4: Chemistry Department, University of Sydney, Sydney, NSW, 2001, Australia

Bottom of Form

Abstract:

Sr3MO4F has been synthesized for M=Al and Ga and shown by Rietveld refinement of neutron and synchrotron X-ray powder diffraction data to adopt a layered structure in which the oxygen and fluorine are ordered and located in different layers.

Journal of Solid State Chemistry, Volume 144, Number 1, April 1999 , pp. 228-231(4)