# Synthesis and Evolution of the Crystalline Phases in Ca1-xSrxAl2O4

Prodjosantoso A.K.1, 2; Kennedy B.J.1

1: School of Chemistry, The University of Sydney, Sydney, NSW, 2006, Australia 2: Universitas Negeri Yogyakarta, Yogyakarta, DIY, 55281, Indonesia

Bottom of Form

Abstract:

The preparation and structural properties of the series of oxides Ca1-xSrxAlO4 are described. Using a combination of synchrotron and neutron powder diffraction methods, it is found that the single-phase solid solutions exist only over a very limited range, x<0.35 and x>0.85. Reitveld refinement analysis demonstrated that at intermediate doping levels a complex series of phases are present. The solubility limit of Sr in CaAl2O4 is rationalized in light of the structural studies.

© 2002 Elsevier Science (USA).

DOI: http://dx.doi.org/10.1006/jssc.2002.9715

Journal of Solid State Chemistry, Volume 168, Number 1, October 2002 , pp. 229-236(8)